|  |  |  |  |
| --- | --- | --- | --- |
|  |  | | |
| **Rocznik Ochrona Środowiska** | | |
| Volume 26 | Year 2024 ISSN 2720-7501 | pp. 413-423 |
|  | https://doi.org/10.54740/ros.2024.040 open access | | |
|  | Received: July 2024 Accepted: August 2024 Published: September 2024 | | |

Assessment of the Energy Potential of Plastics as a Component of ANFO-type Explosives

Jolanta Biegańska

**Department of Hydrogen Energy**, Faculty of Energy and Fuels, AGH University of Krakow, Poland https://orcid.org/0000-0003-2356-3247

corresponding author's e-mail: [biega@agh.edu.pl](mailto:biega@agh.edu.pl)

**Abstract:** Many methods have been developed to reduce the environmental impact of plastic waste. New technologies have been developed to make high-temperature utilisation of these wastes possible. A promising method for the unconventional disposal of plastics by detonation was identified. The popular explosive ANFO (Ammonium Nitrate Fuel Oil) is a component mixture of oxidiser (ammonium nitrate) and fuel (diesel fuel). The optimal composition is 94.5% oxidiser and 5.5% fuel – a guarantee of complete and total combustion. Plastics have a chemical composition and oxygen balance similar to fuel oil. It is possible to replace the fuel share in ANFO by adding plastics and using the energy they contain. The amount of energy that can be recovered is high for PE and PP (at the level of 0.6) and PS – 0.5. Using polymers as ANFO components is advantageous for economic reasons – plastic waste will be eliminated during blasting works.

**Keywords:** energy potential, waste plastics, ANFO


1. Introduction

Plastics have been a useful material used in many industries for many years. Approximately 90% of the overall demand for this raw material is met by low-density polyethylene (LDPE), high-density polyethylene (HDPE), polypropylene (PP), polyethylene terephthalate (PET), (polyvinyl chloride) PVC and (polystyrene) PS (Rodrigues et al. 2019).

After the use stage, plastics become waste, and then they are left to be (Mutha et al. 2006, Kuczenski & Geyer 2010, Geyer et al. 2017):

* recycled or reprocessed,
* subjected to thermal disposal (waste-to-energy),
* landfilled.

According to the OECD (OECD 2022), 353 million tonnes of plastic waste was generated globally in 2019, of which only 9% (33 million tonnes) was recycled. According to the OECD scenario, with this waste increasing to 1014 million tonnes by 2060, landfilling will remain the common form of disposal. Compared to other methods, this way of disposing of plastics is projected, as shown in Figure 1.



**Fig. 1.** Projections of plastic waste by disposal method, World (Ritchie et al. 2023)

A similar scenario presents itself for Europe, but in this case, landfilling and incineration are equivalent disposal forms.

Due to the high durability of plastics and the negative environmental impact if left as waste, various management/disposal methods are being developed.


Attention is drawn to the high energy potential contained in these materials, comparable to fossil fuels (coal, oil). Therefore, the case for using plastics and, at the same time, disposing of them in thermal processes is not unexpected.

Attempts have also been made to use these waste substances as components in explosives/blasting materials (BM) (Biegańska et al. 2004, 2005, Biessikirski et al. 2021).

One of the most commonly used explosives (BM) for rock mining in open-pit mines is ANFO (Ammonium Nitrate Fuel Oil) (Mining…, 2021, Global ANFO 2023). It is also used in metal ore mining and construction (tunnelling and demolition). Regarding industrial use, this material has the largest market share at 56%. ANFO's properties, such as safety, low price, and simple production process, favour its widespread use. It was found (Oluwoye et al. 2017) that the optimal composition of ANFO is 94.5% ammonium nitrate and 5.5% fuel oil. When detonating such a mixture, the formation of toxic gases is minimal; ideally, no products that pose a risk to health and safety should be produced.

2. Disposal Methods for Plastics

Reducing plastic waste is the most effective way to clean up the environment. Proper waste management and source reduction is one of the possible steps to achieve this goal. Only some of the many techniques for managing this waste (recycling, landfilling, incineration and bioremediation) have a scientific basis (Pan et al. 2020). Figure 2 illustrates the different methods used to manage plastic waste and shows the new technologies increasingly being implemented.



**Fig. 2.** Different routes for plastic waste management (Kibria et al. 2023)

It has been noted (Garforth et al. 2004) that landfilling polymer waste is an environmental hazard (this type of waste is poorly biodegradable). Their degradation rate is very slow – for most plastics, the half-life is hundreds or thousands of years once buried in the ground. Only LDPE bags have a short half-life – they decompose in 4.6 years (Chamasa et al. 2020).

Much of this waste is in the municipal waste group; therefore, this form of disposal requires additional efforts to operate landfills properly. As can be seen from the diagram in Figure 2, studies are moving towards developing other forms of disposal for this waste.

2.1. Conventional technologies

In this group of methods, the reuse of post-consumer plastics in various forms of recycling (mechanical, biological and thermochemical) is favoured.

Some types of plastics, after preliminary purification, are crushed and – in powdered form – are used as additives in various products (Gao 2002, Song et al. 2012, Briassoulis et al. 2013, Bilewicz et al. 2014, Wucher et al. 2014, Chen et al. 2019, Titone et al. 2024).

It is the simplest form of recycling but requires an energy input for treatment, sorting, transport and processing.

Biological recycling is breaking down plastics into simple substances using microorganisms.

After such processing, the simple substances will integrate (reintegrate) into the natural environment. It is a time-consuming form and requires the selection of bacteria, fungi and similar microorganisms dedicated to specific types of plastics (Shah et al. 2008, 2016, Al-Salem et al. 2010, Fei et al. 2018, Bandopadhyay et al. 2018, A Hosni et al. 2019, Siracusa 2019, Yuan et al. 2020, Chaurasia 2020, Mohanan et al. 2020, Dailin et al. 2022).

The thermochemical recycling method uses various steps to convert plastics to low molecular weight chemical products (Rahimi & García 2017, Garcia & Robertson, 2017, Zeller 2021). They have further applications, and the processes of such recycling are pyrolysis, gasification, thermal cracking and various forms of incineration (Löpez et al. 2010, Bujak 2015, Uekert et al. 2018, Huang et al. 2018, Nanda & Berruti 2021, Maslak 2021). Using the right equipment (suitable combustion chambers, control systems, flue gas treatment systems), this form of plastic conversion allows energy to be recovered in an environmentally safe way. It can be financially profitable (Scott 2007, Eriksson & Finnveden 2009, Thanh et al. 2011).

It was concluded (Hahladakis et al. 2018, Gharde & Kandasubramanian 2019) that thermal decomposition is an important means of chemical recycling of waste plastics – low pollution of the atmosphere, high product utilisation and high value.

2.2. Modern technologies

The state-of-the-art methods include plasma technologies, polymer-modified road asphalt production, pyrolysis and co-firing in a cement kiln.

Plasma pyrolysis is an innovative thermal technology (Pragnesg et al. 2010, Punčochářa et al. 2012), in which plastic waste is converted to simple substances at high temperatures (approx. 1727°C to 9727°C) from 2,000K to 10,000K (under almost anaerobic conditions) with the production of a valuable gas (syngas). It contains simple molecules of CO, H2, CH4 and higher hydrocarbons in small amounts. To increase gas production, argon plasma (in the form of vapour) was used (Sekiguchi & Orimo 2004). It has proved particularly useful for converting PE in granular form.

Hot plasma can be used to destroy toxic substances and is useful for the disposal of plastics containing chlorine – mixed waste can also be disposed of in this way (Smriti et al. 2016). This technology's suitability for destroying waste multilayer plastics has also been demonstrated (Bhawan & Nagar 2016).

Studies have been conducted on the decomposition of plastics using different pyrolysis methods (Slapak et al. 2000, Pionto et al. 2002, Orgianni et al. 2002).

A steam gasification process was designed for PVC plastics. A variation of this process, fluidised bed gasification, was used, where the temperature of the process played a significant role in the gas composition.

An interesting application of plastics was found to improve the rheological properties of asphalt. The addition of plastics to the asphalt mass resulted in, among other things, higher durability and moisture resistance in the final product (Sabadra 2017, Sulyman 2017, Janik et al. 218). On the other hand, the addition of shredded polyethylene bags and aggregate (Kazmi & Rao 2015) has worked well as a binding agent in road construction.

Research has been conducted (Joohari & Giustozzi 2020, Joohari 2021) to increase the durability of asphalt using a hybrid polymer – elastomer and plastomer. This combination proved a good solution (the high temperature did not affect the phase separation between polymers and asphalt).

Plastic waste has also been used as fuel in cement production in co-processing cement kiln technology (Poddar & Paranjpe 2015, Baidya et al. 2016, Ghosh & Ansari 2019, Prakash & Palkar 2023). The research aimed to recover the energy contained in plastics and simultaneously dispose of them in an environmentally friendly manner. Co-firing of polyethylene waste (with coal or petroleum coke) in cement kilns allows partial replacement of conventional fuels and has no negative environmental impact. The temperature in the cement firing process ranges from 1,123.15K to 2,073.15K (850°C to 1800°C), allowing the plastics to burn completely without forming harmful gases. The products of the process are NaCl, KCl and CaSO4. It was also found that such a process has no negative effect on the properties of the clinker.

It has been shown, using the so-called discrete dynamic programming (Amsaveni et al. 2020), that, in the cement industry, plastics are a raw material that can be maximised through co-processing.

Life-cycle assessment studies (Cement 2021) have shown that this is a better alternative than storing and incinerating plastics. In India, several plants have been set up that specialise in processing waste plastics in such processes (Ultra Tech 2021). In Japan, investments are also being made to build plants for greater use of waste plastics in the process mentioned above (Compendium of Technologies 2021).

In the group of modern technologies, a variant of pyrolysis leads to the production of liquid fuel from waste plastics. Ultra-fast pyrolysis (flash pyrolysis) is an extremely fast thermal decomposition whose main products are gas and bio-oil. The heating rate can range from 100 to 10,000°C/s, and the residence time of the waste in the reactor is short – a few seconds (Eze et al. 2021).

Various facilities for so-called fast pyrolysis have been studied in detail, using the following waste for this purpose: PP, PS, and PET (Namkung 2022). The quality of the oil obtained was in accordance with government regulations (in this case, the Korean ones) where the work was carried out.

Different reactor designs were developed to improve the efficiency of the pyrolysis process (Ahamed et al. 2020, Sharma et al. 2022). A parallel study (Aisien et al. 2021) was carried out to compare thermal and catalytic pyrolysis. It was found that thermal pyrolysis yielded a maximum liquid oil content of 83.3 wt.%.

Microwave-assisted continuous pyrolysis (Zhou et al. 2021) proved an interesting approach, with the highest liquid product yield obtained at 833.15K (560°C).

Thermolysis, as a special case of pyrolysis (Panda et al. 2010, Idumah 2022), has been used successfully to obtain liquid oil – the need for its purification was highlighted. This product could be a future fuel alternative.

3. The Energy Potential of Plastics

Among the methods discussed for the disposal of plastics, various forms of incineration are highlighted as a radical way. Thermal methods allow energy recovery, i.e. the use of waste with a high energy value, which also fits into the hierarchy of waste management and the Zero Waste concept (EU 2008, Cole et al. 2014).

**3.1. Net calorific value of plastics**

The thermal properties of a substance's suitability for energy recovery are determined by its chemical composition, and the most important quantities characterising the amount of heat generated in the combustion process are:

* heat of combustion – HHV (High Heating Value): the amount of heat given off by the complete and total combustion of a unit quantity of fuel after cooling the gaseous products to the initial temperature of the substrates and condensing the water vapour from the flue gases,
* net calorific value – LHV (Low Heating Value): the difference between the heat of combustion and the heat of vaporisation of water released from the fuel during combustion; the net calorific value is lower than the heat of combustion by the amount of the heat of condensation of the water vapour contained in the flue gas.

Plastics are a favourable energy source due to their high calorific value. According to estimates (Villanueva & Eder 2014, Stegmann et al. 2022), the average LHV for plastics is 35 MJ/kg. This is derived from the average value of this parameter calculated, based on literature data, for each type of plastic multiplied by its global market share.

It was assumed (Geyer et al. 2017) that the global market share of each plastic type is for:

* PP 19%,
* LDPE 18%,
* HDPE 15%,
* PP&A (polyester, polyamide and polyacrylic) 14%,
* PVC 11%,
* PET 9%,
* PU (polyurethane) 7% and
* PS 7%.


Based on literature data, the following LHVs (lower heating values) for the different types of plastics have been determined (Table 1).

**Table 1.** Average lower heating values (LHV) per plastic type

|  |  |  |  |
| --- | --- | --- | --- |
| Polymer | Calorific value LHV\*  MJ/kg | LHV\*\*  MJ/kg | Reference |
| Polyethylene (PE) | 43.3 | 43.35 | (Chielini & Solaro 2003) |
| 47.7 | 41.44 | (Walters et al. 2000) |
| Polypropylene (PP) | 42.6 | 43.19 | (Babrauskas 1992) |
| 46.5 | (Tsiamis & Castaldi 2016, FAL 2011) |
| Polystyrene (PS) | 41.6 | 40.19 | (Lechner 2005) |
| 43.7 | (Walters et al. 2000) |
| Polyvinyl chloride (PVC) | 18.0 | 19.69 | (Chielini & Solaro 2003, Tsiamis & Castaldi 2016, FAL 2011, TNO 2020) |
| 19.0 | (Courtemanche & Levendis 1998,  Shi 2015, Lechner 2005) |
| Polyethylene terephthalate (PET) | 21.6 | 23.15 | (Lechner 2005) |
| 24.2 | (Walters et al. 2000) |
| Polyurethane (PU) foam | 31.6 | 26.53 | (RNS 2010) |

\*lower and higher limits, \*\*average of the plastic's share in the world market

Considering the chemical structure of plastics (Figure 3), it should be noted that they are mainly composed of carbon and hydrogen (except for PVC), which, if burned, will not burden the atmosphere with toxic reaction products.



**Fig. 3.** Molecular structures of some of the commonly encountered polymers (Monkul & Özhan 2021,   
Sharma & Vuppu 2023)

Incineration of waste plastics is viable and can replace fossil fuels – similar chemical structure to fuel oil and comparable (to polyethylene, polypropylene or polystyrene) net calorific value of 42-46 MJ/kg.

Currently, an acceptable process for treating plastic waste is incineration in cement kilns.

3.2. Recoverable energy from plastics

The net calorific value of plastics is a kind of determinant of the desirability of thermal disposal of waste from these materials. Before carrying out such a process, an important piece of information is a signal of how much energy can be recovered. Information on the proportion of energy used in the production of plastics is useful in this case, as the quotient of the net calorific value and the total energy consumption in the production of the product is the amount of energy that can be recovered (Marczak 2019).

In analyses of this type, when considering the total energy consumption for the production of a product, so-called raw material energy (energy obtained from crude oil – the raw material for the production of polymers) and process energy (energy used as fuel in processing – the production of plastics from monomers, i.e., e.g. polymerisation) are included.

Given the data (Table 2) on total energy consumption for plastic production, the amount of recoverable energy was calculated. Due to the different data (often inconsistent), certain assumptions were made in the calculations:

* the literature data are for Europe (Plastics Europe 2023, Karali et al. 2024),
  + in the column "Energy consumption", the average value is rounded to the nearest whole number,
  + in the column "Net calorific value", the average value is taken from Table 1 (according to literature data) and rounded up to a whole number.

**Table 2.** Energy recovery in relation to its consumption in the production of selected plastics

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Polymer | Energy  consumption MJ/kg | Calorific value LHV MJ/kg | Part of the recoverable energy | Reference |
| Polyethylene (PE) | 80 | 46 | 0.6 | (Thiriez & Gutowski 2006,  Vlachopoulos 2009,  Iwko & Wróblewski 2019,  Plastics Europe 2023) |
| Polypropylene (PP) | 78 | 45 | 0.6 | (Gervet & Nordell 2007,  Plastics Europe 2023) |
| Polistyrene (PS) | 84 | 43 | 0.5 | (Engelbeen 2022,  Plastics Europe 2023,  Karali et al. 2024) |
| Polyvinyl  chloride (PVC) | 59 | 19 | 0.3 | (Thiriez & Gutowski 2006,  Plastics Europe 2023) |
| Polyethylene  terephthalate (PET) | 71 | 23 | 0.3 | (Plastics Europe 2023,  Karali et al. 2024) |
| Polyurethane (PU) | 94 | 32 | 0.3 | (Plastics Europe 2023) |

As the table shows, the highest data quotient (net calorific value and energy consumption) was obtained for PE and PP, with a value of 0.6. A high result was also obtained for PS, with a value of 0.5. Identical results were achieved for PVC, PET and PU, but with a slightly lower level.

It can be concluded that waste plastics will be an important source of energy that can be used in thermal technologies.

4. Concept for Harnessing the Energy Potential of Plastics

One of the thermal methods preferred for the disposal of waste plastics is incineration in cement kilns. Temperatures as high as 2073.15K (1800°C) in this process allow the plastics to burn completely – without the formation of harmful gases.

Much higher temperatures are reached during the detonation of the explosive, which can guarantee the complete and total combustion of such waste. During the explosive transformation of 1 kg of a BM, the temperature of the resulting gases reaches 4500K (4226.85°C) and energy from 2000-6000 kJ is released (Urbański 1954).

Commonly used blasting materials have lower detonation temperatures, on the order of 2500-3300K (2226.85-3026.85°C) for emulsion BMs (Silvestrov et al. 2014) and 2689-2861K (2415.85-2587.85°C) for ANFOs (Štimac et al. 2020), depending on charge diameter, pressure and detonation conditions. Their explosive decomposition results in reaching already high-temperature values, which is important for the thermal disposal of plastics.

Eliminating the wastes mentioned above by utilising their energy potential in explosive compositions would involve their use as additives in ANFO. Given the simple two-component explosive of this type (ammonium(V) nitrate and fuel oil), modification of its chemical composition is easy and reasonable.

Computer simulations carried out in the EXPLO5 programme (Sućeska 2001, Vasilescu et al. 2020) show the feasibility of designing different mixtures with the calculation of their thermodynamic parameters. Calculations are based on chemical formulae, heat of formation and density.

Although the method of plastic disposal by detonation is unconventional, preliminary studies and theoretical foundations (calculations of thermodynamic properties of modified mixtures) prove that it can be a promising form of plastic waste management (Biegańska & Barański 2017, 2018, Biegańska et al. 2018 a, 2018 b, Biegańska et al. 2022).

5. Conclusions

1. The unconventional method of disposal of plastics, which adds them as components of an explosive, results in disposal through a detonation process.
2. It is possible to replace the share of oil in ANFO with the addition of plastics and use the energy contained in them. The amount of energy that can be recovered is high for PE and PP (at 0.6) and PS – 0.5.
3. Implementing the explosive disposal method on an industrial scale (in mining) can be an alternative and cost-effective method for combustion processes.

*Funding: The publication was implemented as part of the statutory work 16.16.210.476.*

References

Ahamed, A., Veksha A., Yin K., Weerachanchai P., Giannis A., Lisak G. (2020). Environmental impact assessment of converting flexible packaging plastic waste to pyrolysis oil and multi-walled carbon nanotubes. *Journal of Hazardous Materials*, *390*, 121449. <https://dx.doi.org/10.1016/j.jhazmat.2019.121449>

Aisien, E.T., Otuya, I.C., Aisien, F.A. (2021). Thermal and catalytic pyrolysis of waste polypropylene plastic using spent FCC catalyst. *Environmental Technology & Innovation*, *22*, 101455. <https://doi.org/10.1016/j.eti.2021.101455>

Al Hosni, A.S.K., Pittman, J., Robson, G. (2019). Microbial degradation of four biodegradable polymers in soil and compost demonstrating polycaprolactone as an ideal compostable plastic. *Waste Management*, *97*, 105-114. <https://doi.org/10.1016/j.wasman.2019.07.042>

Al-Salem, S.M., Lettieri, P., Baeyens, J. (2010). The valorisation of plastic solid waste (PSW) by primary to quaternary routes: From reuse to energy and chemicals. *Progress in Energy and Combustion Science*, *36*(1), 103-129. <https://doi.org/10.1016/j.pecs.2009.09.001>

Amsaveni, D., Ghayathri, D.K., Venkatesan, S. (2020). Optimising the usage of plastic waste in cement industry using discrete dynamic programming. *Materials Today: Proceedings*, *21*, 257-262. <https://doi.org/10.1016/j.matpr.2019.05.424>

Babrauskas, V. (1992). Heat of Combustion and Potential Heat. In: Heat Release in Fires. Babrauskas, V., Grayson S.J. (Eds.). *Elsevier Applied Science*, London. <https://www.researchgate.net/publication/246363103_Heat_Release_in_Fires>, 207-223.

Baidya, R., Ghosh, S.K., Parlikar, U.V. (2016). Co-processing of industrial waste in cement kiln – a robust system for material and energy recovery. *Procedia Environmental Sciences*, *31,* 309-317. <https://doi.org/10.1016/j.proenv.2016.02.041>

Bandopadhyay S., Martin-Closas L., Pelacho A.M., DeBruyn J.M. (2018). Biodegradable plastic mulch films: impacts on soil microbial communities and ecosystem functions. *Frontiers in Microbiology*, *9*, 819. <https://doi.org/10.3389/fmicb.2018.00819>

Bhawan, P., Nagar, E.A. (2016). Central Pollution Control Board (Ministry of Environment & Forests & Climate Change). Study on Plastic Waste Disposal through "Plasma Pyrolysis Technology". Delhi-110032.

Biegańska, J., Barański, K. (2017). Effect of plastic waste additives on the energetic parameters of ANFO explosives. *High Energy Materials*, *9*, 145-158. <https://doi.org/10.22211/matwys/0153>

Biegańska, J., Barański, K. (2018). Effect of plastic waste additives on the energetic parameters of ANFO explosives. *Tworzywa Sztuczne w Przemyśle*, *4*, 48-54.

Biegańska, J., Barański, K., Tumen-Ulzii, G. (2018a). Influence of the addition of plastics on the content of post-detonation gaseous products of ANFO explosive. *High Energy Materials*, *10*, 5-12. <https://doi.org/10.22211/matwys/0164>

Biegańska, J., Barański, K., Tumen-Ulzii, G. (2018b). Influence of the addition of plastics on the content of gaseous products generated after detonation of ANFO explosive. *IPOEX 2018*: 15th international conference: explosives - research - application - safety. Ustroń Zawodzie 11-13 czerwca 2018 r.

Biegańska, J., Barański, K., Hebda, K., Pytlik, M. (2022). Thermodynamic assessment of the impact of selected plastics on the energy parameters of explosives. *Energies*, *15,* 9583. <https://doi.org/10.3390/en15249583>

[Biegańska](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=02&V_00=Biega%F1ska+Jolanta*+), J., [Olek](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=02&V_00=Olek+J+), J., [Brodowiak](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=02&V_00=Brodowiak+J+), J. (2004). Possibility of use of plastic waste as an energy source. [*Termiczne unieszkodliwianie odpadów*](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=06&V_00=Termiczne+unieszkodliwianie+odpad%F3w+)*. Procesy termiczne w gospodarce odpadami w regionach przyrodniczo-cennych.*   
251-266. Praca zbiorowa. Pod red. Janusza W. Wandrasza. Polskie Zrzeszenie Inżynierów i Techników Sanitarnych. Oddział Wielkopolski, Poznań. (in Polish)

[Biegańska](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=02&V_00=Biega%F1ska+Jolanta*+), J., [Olek](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=02&V_00=Olek+J+), J., [Matyszkiewicz](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=02&V_00=Matyszkiewicz+B+), B. (2005). The application of waste plastics as a modifier of emulsion properties of explosives. [*Paliwa z odpadów*](http://www.bg.polsl.pl/expertusbin/expertus.cgi?KAT=%2Fvar%2Fwww%2Fbibgl%2Fexpertusdata%2Fpar%2F&FST=data.fst&FDT=data01.fdt&ekran=ISO&lnkmsk=2&cond=AND&mask=2&F_00=06&V_00=Paliwa+z+odpad%F3w+)*. T. 5*. Praca zbiorowa pod red. Janusza W. Wandrasza, Krzysztofa Pikonia. Helion, Gliwice, 227-232. (in Polish)

Biessikirski, A., Czerwonka, D., Biegańska, J., Kuterasiński, Ł., Ziąbka, M., Dworzak, M., Twardosz, M. (2021).Research on the possible application of polyolefin waste-derived pyrolysis oils for ANFO manufacturing*. Energies*, *14*,172*.* <https://doi.org/10.3390/en14010172>

Bilewicz, M., Labisz, K., Tański, T., Konieczny, J., Górniak, M. (2014). Structural identification of polymer nanocomposites. *Acta Physica Polonica A*, *126*(4), 895-901. <https://doi.org/10.12693/APhysPolA.126.895>

Briassoulis, D., Hiskakis, M., Babou, E. (2013). Technical specifications for mechanical recycling of agricultural plastic waste. *Waste Management*, *33*(6), 1516-1530. <https://doi.org/10.1016/j.wasman.2013.03.004>

Bujak, J.W. (2015), Thermal utilisation (treatment) of plastic waste. *Energy*, *90*(2), 1468-1477. <https://doi.org/10.1016/j.energy.2015.06.106>

Cement: A plastic positive industry. (2021). *Cement Manufacturers' Association*. December 30, 2021. <https://www.cmaindia.org/cement-plastic-positive-industry>

Chamas, A., Moon, H., Zheng, J., Qiu, Y., Tabassum, T., Jang, J.H., Abu-Omar, M., Scott, S.L., Suh S. (2020). Degradation rates of plastics in the environment. *ACS Sustainable Chemistry & Engineering*, *8*(9), 3494-3511. <https://pubs.acs.org/doi/epdf/10.1021/acssuschemeng.9b06635>

Chaurasia, M. (2020). Analytical review on biodegradation of plastics. *eLifePress*, *1*(1), 1-8. <https://elifepress.com>

Chen R., Li Q., Xu X., Zhang D. (2019). Comparative pyrolysis characteristics of representative commercial thermosetting plastic waste in inert and oxygenous atmosphere. *Fuel*, *246*(1), 212-221. <https://doi.org/10.1016/j.fuel.2019.02.129>

Chiellini, E. & Solaro R. (2003). *Biodegradable polymers and plastics*. New York: Springer Science+Business Media. <https://link.springer.com/content/pdf/10.1007/978-1-4419-9240-6.pdf>

Cole, C., Osmani, M., Quddus, M., Wheatley, A., Kay, K. (2014). Towards a Zero Waste Strategy for an English Local Authority. *Resources Conservation and Recycling*, *89*, 64-75. <https://doi.org/10.1016/j.resconrec.2014.05.005>

Compendium of Technologies for Plastic Waste Recycling and Processing. (2021). IGES Centre Collaborating with UNEP on Environmental Technologies (CCET) and ICLEI – Local Governments for Sustainability. <https://southasia.iclei.org/wp-content/uploads/2022/05/Technology_Compendium_Designed_Final.pdf>

Courtemanche, B., Levendis, Y.A. (1998). A laboratory study on the NO, NO2, SO2, CO and CO2 emissions from the combustion of pulverised coal, municipal waste plastics and tires. *Fuel*, *77*(3), 183-196. <https://doi.org/10.1016/S0016-2361(97)00191-9>

Dailin, D.J., Rithwan, F., Hisham, A.M., Rasid, Z.I.A., Azelee, N.I.W., Sapawe, N., Chuah, L.F., Yusof, A.H.M., Enshasy, H.E. (2022). A Review on current status of plastic waste biodegradation using microbial approach. *Bioscience Research*, *19*(3), 1599-1606. <https://www.researchgate.net/publication/363263600>

Engelbeen, F. (2022). Plastics – Environmental aspects. Indian Institute of Science Centre for Ecological Sciences. <http://ces.iisc.ernet.in/hpg/envis/plasdoc612.html>

Eriksson O., Finnveden G. (2009). Plastic waste as a fuel-CO2-neutral or not? *Energy & Environmental Science*, *2*(9), 907-914. <https://doi.org/10.1039/b908135f>

EU. (2008). Revised Waste Framework Directive, 2008/98/EC.   
<https://eur-lex.europa.eu/legalcontent/EN/TXT/?uri=CELEX%3A32008L0098>

Eze, W.U., Umunakwe, R., Obasi, H.Ch., Ugbaja, M.I., Uche, C.Ch., Madufor, I.Ch. (2021). Plastics waste management: A review of pyrolysis technology. *Clean Technologies and Recycling*, *1*(1), 50-69. <https://doi.org/10.3934/ctr.2021003>

FAL. (2011). Cradle-to-gate life cycle inventory of nine plastic resins and two polyurethane precursors. Revised Final Report. Prepared for the Plastics Division of The American Chemistry Council Prairie Village, KS: Franklin Associates, Ltd. Available at: <http://plastics.americanchemistry.com/LifeCycle-Inventory-of-9-Plastics-Resins-and-4-Polyurethane-Precursors-Rpt-Only>

Fei, F., Wen, Z., Huang, S., De Clercq, D. (2018). Mechanical biological treatment of municipal solid waste: energy efficiency, environmental impact and economic feasibility analysis. *Journal of Cleaner Production*, *178*, 731-739. <https://doi.org/10.1016/j/jclepro.2018.01.060>

Gao, F. (2002). *Handbook of plastics recycling*. F La Mantina (ed). Rapra Technology, Shrewsbury UK. <https://doi.org/10.1002/pi.1323>

Garcia, J.M., Robertson, M.L. (2017). The future of plastics recycling. *Science*, *358*(6365), 870-872. <https://doi.org/10.1126/science.aaq0324>

Garforth, A.A., Ali, S., Hernández-Martínez, J., Akah, A. (2004). Feedstock recycling of polymer wastes. *Current Opinion in Solid State and Materials Science*, *8*(6), 419-425. <https://doi.org/10.1016/j.cossms.2005.04.003m>

Gervet, B. & Nordell, B. (2007). The use of crude oil in plastic ma king contributes to global warming. Renewable Energy Research Group Division of Architecture and Infrastructure Luleå University of Technology SE-97187 Luleå, Sweden. <https://www.researchgate.net/publication/266469821>

Geyer, R., Jambeck, J.R., Law, K.L. (2017). Production, use, and fate of all plastics ever made. *Science* *Advances*, *3*(7), 1-5. <https://doi.org/10.1126/sciadv.1700782>

Gharde S., Kandasubramanian B. (2019). Mechanothermal and chemical recycling methodologies for the fibre reinforced plastic (FRP). *Environmental Technology & Innovation*, *14*, 100311. <https://doi.org/10.1016/j.eti.2019.01.005>

Ghosh D.S., Ansari S.A. (2019). An investigation on process optimisation in cement industries through Co-processing of plastic waste. *International Journal of Modern Engineering & Management Research*, *7*(4), 5-13. <http://www.ijmemr.org/Publication/V7I4/IJMEMR-V7I4-001.pdf>

Global ANFO Grade Ammonium Nitrate Market Research Report 2023.   
<https://reports.valuates.com/market-reports/QYRE-Auto-21K8031/global-anfo-grade-ammonium-nitrate>

Hahladakis, J.N., Velis, C.A., Weber, R., Iacovidou, E., Purnell, P. (2018). An overview of chemical additives present in plastics: migration, release, fate and environmental impact during their use, disposal and recycling. *Journal of Hazardous Matererials*, *344*, 179-199. <https://doi.org/10.1016/j.jhazmat.2017.10.014>.

Huang, J., He, C., Li, X., Pan, G., Tong, H. (2018). Theoretical studies on thermal degradation reaction mechanism of model compound of bisphenol a polycarbonate. *Waste Management*, *71*, 181-191. <https://doi.org/10.1016/j.wasman.2017.10.016>

Idumah, C.I. (2022). Recent advancements in thermolysis of plastic solid wastes to liquid fuel. *Journal of Thermal Analysis and Calorimetry*, *147*, 3495-3508. <https://doi.org/10.1007/s10973-021-10776-5>

Iwko, J., Wróblewski, J. (2019). Experimental study on energy consumption in the plasticising unit of the injection molding machine. *International Scientific Journal "Industry 4.0"*, *4*(5), 241-245.

Janik, H., Sienkiewicz, M., Borzędowska-Labuda, K. (2018). Polymer modified bitumen. *IX International Scientific-Technical Conference: Advance in PEtroleum and Gas Industry and Perochmistry*, 14-17. <https://mostwiedzy.pl/en/publication/polymer-modified-bitumen,145259-1>

Joohari, I.B., Giustozzi, F. (2020). Hybrid polymerisation: An exploratory study of the chemo-mechanical and rheological properties of hybrid-modified bitumen. *Polymers*, *12*(4), 945. <https://doi.org/10.3390/polym12040945>

Joohari, I.B. (2021). Development of hybrid polymer modified bitumen for road pavement applications. *Dissertation.*1-239.Royal Melbourne Institute of Technology, Australia.

Karali, N., Khanna, N., Shah, N. (April 2024). *Climate Impact of Primary Plastic Production. Sustainable Energy and Environmental Systems Department*. Lawrence Berkeley National Laboratory*.* 109. <https://escholarship.org/uc/item/6cc1g99q>

Kazmi, S., Rao, D.G. (2015). Utilisation of waste plastic materials as bitumen-blends for road construction in Oman*.* *Scholars Journal* *of Engineering and Technology*, *3*(1A), 9-13. <https://saspublishers.com/article/2598/download/>

Kibria, M.G., Masuk, N.I., Safayet, R., Nguyen, H.Q., Mourshed, M. (2023). Plastic waste: challenges and opportunities to mitigate pollution and effective management. *International Journal of Environmental Research*, *17*(1), 20. <https://doi.org/10.1007/s41742-023-00507-z>

Kuczenski, B., Geyer, R. (2010). Material flow analysis of polyethylene terephthalate in the US, 1996-2007. *Resources, Conservation and Recycling*, *54*(12), 1161-1169. <https://doi.org/10.1016/j.resconrec.2010.03.013>

Lechner, M.D. (2005). Polymers. In: *Springer Handbook of Condensed Matter and Materials Data.* (Eds.) Martiensen, W., Warlimont, H. On line at: <http://www.springer.com/978-3-540-44376-6>, 477-522.

Löpez, A., de Marco, I., Caballero, B.M., Laresgoiti, M.F., Adractos, A. (2010). Pyrolysis of municipal plastic wastes: influence of raw material composition. *Waste Management*, *30*(4), 620-627. <https://doi.org/10.1016/J.wasman.2009.10.014>

Marczak, H. (2019). Analysis of the energetic use of fuel fractions made of plastic waste. *Journal of Ecological Engineering*, *20*(8), 100-106. <https://doi.org/10.12911/22998993/110766>

Maslak, Anastasia L. (2021).Thermochemical conversion of plastic to value added products. *Electronic Thesis and Dissertation Repository*. 8299. <https://ir.lib.uwo.ca/etd/8299>

Mining Explosives Market Insights, 2031. (2021). <https://www.transparencymarketresearch.com/mining-explosives-market.html>

Mohanan, N., Montazer, Z., Sharma, P.K., Levin, D.B. (2020). Microbial and enzymatic degradation of synthetic plastics. *Frontiers in Microbiology*, *11*, 580709. <https://doi.org/10.3389/fmicb.2020.580709>

Monkul, M.M. & Özhan, H.O. (2021). Microplastic contamination in soils: A review from geotechnical engineering view. *Polymers*, *13*, 4129. <https://doi.org/10.3390/polym13234129>

Mutha, N.H., Patel, M., Premnath, V. (2006). Plastics material flow analysis for India. *Resources, Conservation and Recycling*, *47*(3), 222-244. <https://doi.org/10.1016/j.resconrec.2005.09.003>

Namkung, H., Park, S.-I., Lee, Y., Han, T.U., Son, J.-I., Kang, J.-G. (2022). Investigation of oil and facility characteristics of plastic waste pyrolysis for the advanced waste recycling policy. *Energies*, *15*, 4317. <https://doi.org/10.3390/en15124317>

Nanda, S., Berruti, F. (2021). Thermochemical conversion of plastic waste to fuels: a review. *Environmental Chemistry Letters*, *19*, 123-148. <https://doi.org/10.1007/s10311-020-01094-7>

OECD (2022). *Global Plastics Outlook: Policy Scenarios to 2060*, OECD Publishing, Paris. <https://doi.org/10.1787/aa1edf33-en>

Oluwoye, I., Dlugogorski, B.Z., Gore, J., Okierski, H.C., Altarawneh, M. (2017). Atmospheric emission of NOx from mining explosives: A critical review. *Atmospheric Environment*, *16*(167), 81-96. <https://doi.org/10.1016/j.atmosenv.2017.08.006>

Orgianni, C., De Filippis, P., Pochetti, F., Paolucci, M. (2002). Gasification process of waste containing PVC. *Fuel*, *81*(14), 1827-1833.<https://doi.org/10.1016/S0016-2361(02)00097-2>

Pan, D., Su, F., Liu, Ch., Guo, Z. (2020). Research progress for plastic waste management and manufacture of value-added products. *Advanced Composites and Hybrid Materials*, *3*(4), 443-461.   
<https://doi.org/10.1007/s42114-020-00190-0>

Panda, A.K., Singh, R.K., Mishra, D.K. (2010). Thermolysis of waste plastics to liquid fuel a suitable method for plastic waste management and manufacture of value added products – a world prospective. *Renewable and Sustainable Energy Reviews*, *14*(1), 233-248. <https://doi.org/10.1016/j.rser.2009.07.005>

Pinto, F., Franco, C., Andre, R.N., Miranda, M., Gulyutlu, I., Cabrita, I. (2002). Co-gasification study of biomass mixed with plastic waste. *Fuel*, *81*, 291-297. <https://api.semanticscholar.org/CorpusID:93399055>

Plastics Europe. (2023). Eco-profiles for determining environmental impacts of plastics. <https://plasticseurope.org/sustainability/circularity/life-cycle-thinking/eco-profiles-set/>

Poddar S.K., Paranjpe A. (2015). Energy recovery through plastic waste in cement industry: A review. *International Journal of Recent Development in Engineering and Technology*, *4*, 15-18. <https://www.ijrdet.com/files/Volume4Issue5/IJRDET_0515_03.pdf>

Pragnesh N Dave, Asim K Joshi. (2010). Plasma pyrolysis and gasification of plastics waste – A review. *Journal of Scientific & Industrial Research*, *69*(3), 177-179. <https://www.researchgate.net/publication/229020408>

Prakash, A., Palkar, R.R. (2023). Co-processing of plastic waste in a cement kiln: a better option. *Environmental Science and Pollution Research*, *30*, 24804-24814. <https://doi.org/10.1007/s11356-021-17725-7>

Punčochářa, M., Ruj, B., Chatterjee, P.K. (2012). Development of process for disposal of plastic waste using plasma pyrolysis. *Procedia Engineering*, *42*, 420-430. <https://doi.org/10.1016/j.proeng.2012.07.433>

Rahimi, A., García, J. (2017). Chemical recycling of waste plastics for new materials production. *Nature Reviews Chemistry*, *1*, 0046. <https://doi.org/10.1038/s41570-017-0046>

Ritchie, H., Samborska, V., Roser, M. (2023). Plastic pollution. Published online at: *OurWorldInData.org.* <https://ourworldindata.org/plastic-pollution>

RNS. Romanian National Standard. (2010). SR EN ISO 1716. Fire standard for construction materials, Determining the gross calorific value of solid fuels (in Romanian). <https://cdn.standards.iteh.ai/samples/45780/c4160d8dec954762800c181854e7672f/ISO-1716-2010.pdf>

Rodrigues, M.O., Abrantes, N., Goncalves, F.J.M., Nogueira, H., Marques, J.C., Gonçalves, A.M.M. (2019).Impacts of plastic products used in daily life on the environment and human health: What is known? *Environmental Toxicology and Pharmacology*, *72*, 103239. <https://doi.org/10.1016/j.etap.2019.103239>

Sabadra, V. (2017). Use of polymer modified bitumen in road construction. *International Research Journal of Engineering and Technology*, *04*(12),799-801*.* <https://www.irjet.net/archives/V4/i12/IRJET-4I12152.pdf>

Scott, G. (2007). *Polymers and the Environment*. Royal Society of Chemistry, London. <https://doi.org/10.1039/9781847551726>

Sekiguchi, H., Orimo, T. (2004). Gasification of polyethylene using steam plasma generated by microwave discharge. *Thin Solid Films*, *457*(1), 44-47. <https://doi.org/10.1016/j.tsf.2003.12.035>

Shah, A.A., Hasan, F., Hameed, A., Ahmed, S. (2008). Biological degradation of plastics: a comprehensive. *Biotechnology Advances*, *26*(3), 246-265. <https://doi.org/10.1016/j.biotechadv.2007.12.005>

Shah, Z., Gulzar, M., Hasan, F., Shah, A.A. (2016). Degradation of polyester polyurethane by an indigenously developed consortium of Pseudomonas and Bacillus species isolated from soil. *Polymer Degradation and Stability*, *134*(4), 349-356. <https://doi.org/1016/j/polymdegradstab.2016.11.003>

Sharma, N., Vuppu, S. (2023). In silico study of enzymatic degradation of bioplastic by microalgae: An outlook on microplastic environmental impact assessment, challenges, and opportunities. *Molecular Biotechnology September*, *27*. <https://doi.org/10.1007/s12033-023-00886-w>

Sharma, V., Hossain, A.K., Griffiths, G., Duraisamy, G., Krishnasamy, A., Ravikrishnan, V., Sodré, J.R. (2022). Plastic waste to liquid fuel: A review of technologies, applications, and challenges. *Sustainable Energy Technologies and Assessments*, *53*(C), 102651. <https://doi.org/10.1016/j.seta.2022.102651>

Shi, H. (2015). *Characterisation, heating value modeling and pyrolysis studies of municipal solid wastes*. University Press: Calgary. 106. <http://dx.doi.org/10.11575/PRISM/25264>

Silvestrov, V.V., Bordzilovskii, S.A., Karakhanov, S.M., Plastinin A.V. (2014). On possibility of detonation products temperature measurements of emulsion explosives. *Archives of Metallurgy and Materials*, *59*(3), 1151-1154. <https://doi.org/10.2478/amm-2014-0200>

Siracusa, V. (2019). Microbial degradation of synthetic biopolymers waste. *Polymers*, *11*(6), 1066-1083. <https://doi.org/10.3390/polym11061066>

Slapak, M.J.P., van Kasteren, J.M.N., Drinkenburg, A.A.H. (2000). Design of a process for steam gasification of PVC waste. *Resources Conservation and Recycling*, *30*(2), 81-93. <https://doi.org/10.1016/S0921-3449(00)00047-1>

Smriti D., Richa, D. Kulshrestha, D.A. (2016). Role of plasma in disposing the plastic. *International Journal of Pure and Applied Researches*, *3*(1), 11-17. <https://api.semanticscholar.org/CorpusID:208342469>

Song, S.X., Hu, J., Wu, Z.W. (2012). The pulverisation and its dynamic model of waste thermosetting phenol-formaldehyde resins. *Applied Mechanics and Materials*, *130-134*, 1470-1474. [https://doi.org/10.4028/www.scientific.net/AMM.130-134.1470](https://doi.org/10.4028/www.scientific.net/AMM.130-134.1470%20)

Stegmann, P., Daioglou, V., Londo, M., Junginger, M. (2022). The plastics integrated assessment model (PLAIA): Assessing emission mitigation pathways and circular economy strategies for the plastics sector. *MethodsX*, *9*(2), 101666. <https://doi.org/>[10.1016/j.mex.2022.101666](http://dx.doi.org/10.1016/j.mex.2022.101666)

Štimac, B., Škrlec, V., Dobrilović, M., Sućeska, M. (2020). Numerical modelling of non-ideal detonation in ANFO explosives applying Wood-Kirkwood theory coupled with EXPLO5 thermochemical code. *Defence Technology*, *17*(5), 1740-1752.<https://doi.org/10.1016/j.dt.2020.09.014>

Sućeska, M. (2001). EXPLO5 – Computer program for calculation of detonation parameters. *Proc. of 32nd International Annual Conference of ICT. Energetic Materials, Ignition, Combustion and Detonation.* 110.1-110.13.Karlsruhe, Germany. <https://www.researchgate.net/publication/268390920>

Sulyman, M. (2017). Study on polymer modified road asphalt mixture. *Thesis, nostrification*. Gdańsk University of Technology. 1-201. <https://mostwiedzy.pl/en/publication/study-on-polymer-modified-road-asphalt-mixture,155596-1>

Thanh, N.P., Matsui, Y., Fujiwara, T. (2011). Assessment of plastic waste generation and its potential recycling of household solid waste in Can Tho City, Vietnam. *Environmental Monitoring Assessment*, *175*(1-4), 23-35. <https://doi.org/10.1007/s10661-010-1490-8>

Thiriez, A. & Gutowski, T. (2006). An environmental analysis of injection molding. *Proceedings of the 2006 IEEE International Symposium on Electronics and the Environment*. 195-200. Scottsdale, AZ, USA. <https://doi.org/10.1109/ISEE.2006.1650060>

Titone, V., Botta, L., Mistretta, M.C., La Mantia, F.P. (2024). Influence of a biodegradable contaminant on the mechanical recycling of a low-density polyethylene sample. *Polymer Engineering & Science*, *64*(2), 845-851. <https://doi.org/10.1002/pen.26588>

TNO. (2020). Phyllis 2: Database for the physico-chemical composition of (treated) lignocellulosic biomass, micro- and macroalgae, larious leedstocks for liogas production and biochar. Retrieved May 8, 2019. <https://phyllis.nl/>

Tsiamis, D.A., Castaldi M.J. (2016). Determining accurate heating values of non-recycled plastics. City University of New York. <https://www.wtert.net/member/1825/Demetra_Tsiamis.html>

Uekert, T., Kuehnel, M., Wakerley, D., Reisner, E. (2018). Plastic waste as a feedstock for solar-driven H 2 generation. *Energy Environ Science*, *11*(10), 2853-2857. <http://dx.doi.org/10.1039/c8ee01408f>

UltraTech Cement Limited. (2021). Making a material difference. *Sustainability Report 2021-22*. Mumbai, Maharashtra, India. [www.ultratechcement.com](http://www.ultratechcement.com)

Urbański, T. (1954). *Chemistry and technology of explosives.* (in Polish: *Chemia i technologia materiałów wybuchowych)*. Ministerstwo Obrony Narodowej, Warszawa.

Vasilescu, G., Kovacs, A., Gheorghiosu, E., Garaliu, B., Ilcea G. (2020). Numerical simulation for determining detonation parameters of explosive substances using EXPLO5 thermochemical prediction software. *MATEC Web of Conferences, 305*, 00049. 9th International Symposium on Occupational Health and Safety (SESAM 2019). <https://doi.org/10.1051/matecconf/202030500049>

Villanueva, A., Eder, P. (2014). End-of-waste criteria for waste plastic for conversion: Technical proposals. *Environmental Science*. <https://doi.org/10.2791/13033>

Vlachopoulos, J. (2009). An assessment of energy savings derived from mechanical recycling of polyethylene versus new feedstock. *A report prepared for the World Bank. Version 3.2.* Canada. <https://api.semanticscholar.org/CorpusID:219618535>

Walters, R.N., Lyon, R.E., Hackett, S.M. (2000). Heats of combustion of high-temperature polymers. *Fire and Materials*, *24*(5), 245-252. <https://api.semanticscholar.org/CorpusID:39300177>

Wucher B., Lani F., Pardoen T., Bailly Ch., Martiny P. (2014). Tooling geometry optimisation for compensation of cure-induced distortions of a curved carbon/epoxy C-spar. *Composites Part A*, *56*, 27-35. <https://doi.org/10.1016/j.compositesa.2013.09.010>

Yuan, J., Ma, J., Sun, Y., Zhou, T., Zhao, Y., Yu, F. (2020). Microbial degradation and other environmental aspects of microplastics/plastics. *Science of the Total Environment*, *715*, 136968. <https://doi.org/10.1016/j.scitotenv.2020.136968>

Zeller, M., Netsch, M., Richter, F., Leibold, H., Stapf, D. (2021) Chemical recycling of mixed plastic wastes by pyrolysis – pilot scale investigations. *Chemie Ingenieur Technik*, *93*(11), l763-1770. <https://doi.org/10.1002/cite.202100102>

Zhou, N., Dai, L., Lv, Y., Li, H., Deng, W., Guo, F., Chen, P., Lei, H., Ruan, R.R. (2021). Catalytic pyrolysis of plastic wastes in a continuous microwave assisted pyrolysis system for fuel production. *Chemical Engineering Journal*, *418*, 129412. <https://api.semanticscholar.org/CorpusID:233536413>